## Slide 1: Conductivity
Ilya Belopolski, Sheldon Kwok
TAs: Dr. Benjamin Nachumi, Kenneth Sikes
Physics W3081, Professor May

## Slide 2: Introduction
Measure the response of crystalline solids to applied electric fields as a function of temperature
Fundamental properties of solid state systems
Physical basis for modern electronics
Critical temperature of NbTi superconductor
Resistance as a function of temperature in Pt
Curie point and magnetization of Ni
Band gap of Si using a PN junction

## Slide 3: Methods
Low-temperature measurements in helium refrigerator
High-temperature measurements in oven
Measurement setup:

## Slide 4: Methods
Measure small resistances with four-point contact measurement:
Seebeck effect: measurement error due to thermal gradient across leads
Alternate the direction of applied current, take two voltage measurements, and average them
R
I-
I+
V+
V-

## Slide 5: Superconductivity
Below a critical temperature Tc , superconductors carry current without resistance
Low-temperature superconductivity (Tc < 40Κ), predicted by BCS theory (1957)
  Electron-phonon interactions create Cooper pairs
  Cooper pairs form Bose-Einstein condensate, insensitive to disorder, so no resistivity
High-temperature superconductivity (Tc > 40Κ) unexplained, various pairing mechanisms proposed

## Slide 6
Accepted value: 19 K

## Slide 7: Bloch-Grüneisen Conductivity
Assume that resistance due to electron-phonon scattering
Phonons obey Bose-Einstein statistics: different phonon excitation populations at different temperatures
Finite number of possible excitations determined by lattice spacing and crystal size

## Slide 8: Bloch-Grüneisen Conductivity
Debye approximation: assume that the energy of a phonon magnitude of wave vector
Can show that resistivity is given by,
Universal function of
Low temperatures:
High temperatures:

## Slide 9
Accepted value: 230 K

## Slide 10: Conductivity near the Curie Point
Magnetization = difference in # of oppositely polarized electrons
Energetically favorable for electron spins to align
When T is lowered, number of conducting charges (n) increases, and mean free time (τ) increases
Change in resistance below the Curie Point is proportional to the square of the magnetization
where σ is conductivity, q is charge and m is mass

## Slide 11: Curie Point of Nickel
Known Curie Point for Nickel : 631 K

## Slide 12: Magnetization of Nickel

## Slide 13: P-N Junction
Electrons/Negative Carriers
Holes/Positive Carriers
N-Type
P-Type
Conduction Band
Valence Band
Band Gap
x
Majority Negative Carriers Minority Positive Carriers
Majority Positive Carriers Minority Negative Carriers
Positive Potential
Natural Potential Difference (V0) + Applied Potential Difference (V)
n-side
p-side
N type (extra negative carriers), P type (extra positive carriers)

## Slide 14: P-N Junction
x
Minority Positive Carriers
Majority Positive Carriers
Positive Potential
Natural Potential Difference (V0) + Applied Potential Difference (V)
n-side
p-side
For positive carriers
  I0 Independent of applied potential, depends on number of minority carriers
  I1 Needs to overcome potential hill. At V=0, I1 = I0, I1 increases exponentially with V.

## Slide 15: P-N Junction
Current of diode is measured as function of voltage and at different temperatures
Determine I0 at each temperature
Plot of ln(I0) vs 1/T is linear, and slope gives band gap energy of material.

## Slide 16: Band Gap of Silicon

## Slide 17: Band Gap of Silicon

## Slide 18: Sources of Error
Temperature Errors
  Poor Thermal Contact
  Did not reach thermal equilibrium
  Insulation in refrigerator
  Temperature calibration with Platinum
Silicon Band Gap errors
  Seebeck effect
  Temperature drift
Sample impurities, Improperly calibrated thermometers

## Slide 19: Acknowledgements
Professor Morgan May
Dr. Benjamin Nachumi
Kenneth Sikes
Imre Bartos